## Slide 1
Fundamentals of Optoelectronic Materials and Devices
Hsing-Yu Tuan (段興宇）
Department of Chemical Engineering, National Tsing-Hua University
光電材料與元件基礎

## Slide 2: Textbook in this lecture
Optoelectronics and photonics priciples and practices, S.O. Kasap 1999
Solid state electronic devices, Ben G. streetman and sanjay banerjee, fifth edition

## Slide 3
Band gap schematic of Si

## Slide 4
Distinction between insulator, semiconductor and metal
Streetman p62
Insulator Semiconductor Metal
conduction band
valance band
> 5 eV
-very few electrons excited to
valance band at room temperature
-few electrons excited to conduction band
Ex, Si: 1010 / cm3
(note: Si has 5x1022 atoms/cm3)
plenty of
electrons

## Slide 5
Direct band gap and indirect band gap structure

## Slide 6
Semiconductor, band gap, and wavelength
The band gap corresponds to the wavelength
of light that emits from the semiconductor
顏色名 | 波長 (nm)
紫 | 380-450
藍 | 450-495
綠 | 595-570
黃 | 570-590
橙 | 590-620
紅 | 620-750
Eg=1240/λ eV

## Slide 7: Carrier: electron and hole
Some electrons were excited to the conduction band at temperature >0K
For convenience, an empty state in the valence band is referred to as a hole
Electron-hole pair (EHP): conduction band electron and the hole are
created by the excitation of a valence band electron
-EHPs are free charge carriers in semiconductor materials
-Si, at room temperature has 1010 EHP/cm3 (Si: 5x1022 atoms/cm3)

## Slide 8: Doped materials
Donors: P, As, Sb (Column V elements ) , n-type,  provide one additional electron
Acceptors: B, Ga, In, (Column III elements), p-type provide one additional hole
P+
-
B-
-weakly bound
-bonding strength EB~ 0.05 eV (Si bonding ~1.12 eV)
Majority carrier - electron in a n-type material
hole in a p-type material
Minority carrier – hole in a n-type material
electron in a p-type material
n
p
The nomination is not limited to
Si, but for any semiconductors

## Slide 9: Equilibrium distribution of carriers in intrinsic and doped semiconductors
g(E)
hole 1-f(E)
n
Ec
EF
Ei
Ev
Ec
Ei
EF
Ev
fermi level shift
Ec
Ei
Ev
Intrinsic
n-type
p-type
p
i

## Slide 10: R-G statistics
-The rate of change in the carrier concentration
perturbation
△P
n~no
△p<<no
Low level injection implied
△p<<no n~no in an n-type material
△n<<Po p~po in an p-type material
n-type semiconductor
A technical men given to the mathematical characterization of recombination-generation process
R-G evaluates the time rate of change in the carrier concentrations
Ec
ET(R-G)censter
Ev

## Slide 11: n-type semiconductor after a perturbation
t=0
P0
n-type semiconductor
t>0
perturbation
△P
n-type semiconductor
t->infinite
perturbation
△P=0
n-type semiconductor
The change of minority carriers
dominate the recombination rate
Ec
EF
ET(R-G)censter
Ev
n~no
po
△P<<no
To be approximately
Proportional to △P
(R-G)
For holes in a n-type material;
(R-G)
To be approximately
Proportional to NT (R-G center numbers)
For electrons in a
p-type material
(since the multitude of electrons rapidly
fill any level that is vacant)
The more holes available for
annihilation, the greater
the number of holes recombining
per second.
(R-G)
Cp Cn is a positive proportionality constant
(R-G)

## Slide 12: Minority Carrier lifetimes
For holes in an n-type material
For electrons in an p-type material
-are called minority carrier lifetimes ; interpreted as the average time
an excess minority carrier will live in a sea of majority carriers
-In a Si with very few R-G center, lifetime is around 1 msec
- Typical minority carrier lifetimes in most Si device is around 1 μsec
We introduce the time constants
Diffusion lengths
hole in an n-type material
electron in a
p-type material
(R-G)
(R-G)

## Slide 13: Charge neutrality
In a semiconductor with equilibrium state.
the charge should be neutral, otherwises,
there occurs an electric field
qp – qn + qND - qNA = 0
+
-
ND+ = number of positively charged donor sites
NA- = number of negative charged acceptor sites
Charge/cm3

## Slide 14: Carrier Related terminology
Dopants: specific impurity atoms which are added to semiconductors in controlled amounts for the expressed purpose of increasing either the electron or the hole concentration
Intrinsic semiconductor: undoped semiconductor; a semiconductor whose properties are native to the material
Extrinsic semiconductor – doped semiconductor; a semiconductor whose propeties are controlled by added impurity atoms
Donor – impurity atom which increase the electron concentration; n-type dopant.
Acceptor – impurity atom which increase the hole concentration; p-type dopant
N-type material – a donor-doped material; a semiconductor containing more electrons than holes
P-type material – an acceptor-doped material; a semiconductor containing more holes than electrons
Majority carrier – the most abundant carrier in a given semiconductor sample; electrons in an n-type materials, holes in a p-type material.
Minority carrier – the least abundant carrier in a given semiconductor sample; holes in an n-type material, electrons in a p-type material.

## Slide 15: Equilibrium Fermi energy
Space charge in depletion region
Uniformly doped p- and n-type semiconductors before joining
Electric field in the depletion region and the energy band diagram of a p-n junction in thermal equilibrium
When a p-type and a n-type material meet together: PN-Junction
the same as before

## Slide 16: Invariance of the Fermi level at equilibrium
Electrons transfer rate from 1 to 2 is proportional to
Electrons transfer rate from 2 to 1 is proportional to
At equilibrium, not net transfer electrons, so these must be equal
=
EF1=EF2
dEF
dx
=0
In the beginning of diffusion
Empty sites
The number of filled states

## Slide 17: Einstein Relation
Under equilibrium conditions the Fermi level inside a materials (or inside a group of materials in intimate contact) is invariant as a function of position; that is dEF/dx = dEF/dy=dEF/dz=0 under equilibrium conditions

## Slide 18: P-N junction:

## Slide 19: Space charge
Space charge distribution
Rectangular approximation of the space charge distribution
-The n-side near the junction
Becomes depleted of majority carriers
And therefore has exposed positive donor ions
-Similar situation happens to p-side
-The region on both sides of the
junction M consequently becomes
depleted of free carriers in comparison
with the bulk p and n regions,
called – space charge layer, known as
depletion region

## Slide 20: Energy band diagram of an abrupt junction at thermal equilibrium
A p-n junction with abrupt doping changes at the metallurgical junction
There will be a bulit-in voltage created in the junction

## Slide 21
PN junction:summary
E=-dV/dx
charge density
potential
Story:
The carrier concentraion
difference between the n and p
regions causes the carriers to
diffuse. The diffusion, however,
Leads to a charge imbalance.
the charge imbalance in turn
produces an electric field, which
counteracts the diffusion so that
in thermal equilibrium the net
flow of carriers Is zero.
The charged region near the
metallurgical junction where
the mobile carriers have been
reduced is called the depletion
region
Vo: built-in-potential
no carrier in the
depletion region

## Slide 22: Energy band diagram in an applied field
n-type semiconductor
connected to a voltage
The applied voltage makes
the energy band bend and cause
the potential energy difference between
two sides of n-type semiconductor
-EF(A)-EF(B)=eV, meaning the electrostatic
PE barrier between A and B
E=-dV/dx

## Slide 23: Depletion layer width and energy band diagrams of a p-n junction under various biasing conditions
Thermal-equilbrium condition
Forward-bias condition
Reverse-bias condition
The width of depletion layer
can be externally adjusted
by the applied voltage

## Slide 24
Forward and reverse bias effect for a pn junction
Fermi level equilibrium
Forward bias reduces the eVo to
e(Vo-V), so the electrons at Ec
in the n-side can overcome the the
potential barrier and diffuse to the p-side
A reverse bias, V=-Vr, Vr adds to the
built-in potential Vo, so the P.E barrier
becomes e(Vo+Vr), so there is hardly any
reverse current.

## Slide 25: Fabrication of Light Emitting Diode using a pn junction structure

## Slide 26
Light Emitting Diodes: Principle
made by a junction consists of p-side with heavily-n-doped-side (n+)
Depletion region extends mainly into p-side
built in voltage
the recombination of injected electrons in the depletion region as well as in the
neutral p-side and results in spontaneous emission of photons
-the recombination zone is called the active region
-light emission from EHP recombination as a result of minority carrier injection
is called injection electroluminescence

## Slide 27
-P-layer has to be narrow (a few microns) to allow the emitted photons escape
without being reabsorbed
LED device structure
Narrow

## Slide 28
LED device structure
p
GaAs is around 160

## Slide 29
LED device illustration

## Slide 30: LED semiconductor materials
ηexternal = Pout (optical) x 100%
IV
1993 年日亞(Nichia)發展高效率藍光LED!

## Slide 31
LED materials – mainly III-V based direct band gap
materials
- II-VI compounds are hard to be doped, so not usually be used

## Slide 32
Evolution of light source

## Slide 33
Tuning band gap by alloying or doping
y=0.45, λ=630 nm
Red light
Nitrogen doped indirect bandgap GaAs1-yPy allows can emit green, yellow, orange LEDs
Al doped SiC, GaN are can emit blue emission, however, Al doped SiC is indirect band gap
and GaN is very expansive
Alloy
doping

## Slide 34: LED characteristics
The energy of an emitted photon from an LED is not equal to the Eg
Electron (hole) concentration’s peak position is 1/2kBT above Ec or Ev
and direct recombination is proportional to the concentration
-The linewidth is defined as width between half-intensity equal to △hv , normally
is around 2.5-3 kBT
E=hv

## Slide 35
Output spectrum of a red GaAsP LED
- =24 nm is around 2.7kBT
-Turn-on voltage increase with the energy bandgap Eg, vlue LED is 3.5-4.5 V
yellow LED is around 2 V, GaAs infraed LED is around 1 V
Turn-on voltage:1.5V

## Slide 36
Peak emission

## Slide 37: White light LED
White light for lighting – long service life, electricity effective, low driving voltage, safe
White light LED:
First example: Blue LED + YAG (yttrium aluminum garnet, 釔鋁石榴石) yellow phosphor (currently most popular, low cost & high efficiency) (at 1996)
- RGB LEDs (Red:green:blue = 3:6:1)
- UV LED (GaN) + RGB phosphors

## Slide 38: Various combination of white LED

## Slide 39: Evolution of light source
LED has 80% lower energy vs. incandescent
LED has 39% lower energy vs. CFL
Courtesy of Osram
compact fluorescent light
Efficiency now is
the best.

## Slide 40: Light output V.S. Efficiency

## Slide 41: Cost comparison of light bulbs

## Slide 42: Cost comparison of light bulbs

## Slide 43: Is the technology revolution similar?

## Slide 44
High tech product combined with LED
水立方