## Slide 1
Fundamentals of Optoelectronic Materials and Devices
Hsing-Yu Tuan (段興宇）
Department of Chemical Engineering, National Tsing-Hua University
光電材料與元件基礎

## Slide 2: Semiconductor fundamentals
Basic concept :
-Band structure
-Carrier
References:
Optoelectronics and photonics priciples and practices, S.O. Kasap 1999
Solid state electronic devices, Ben G. streetman and sanjay banerjee, fifth edition

## Slide 3
Si: 14 electrons, 10 core electrons (1s22s22p6)
and 4 valence electrons (3s23p2)
Electronic configuration of Si
1s22s22p63s23p2
Hybridation of s-oribitals and
p orbitals
Linear combinations of atomic orbitals
(LCAO)
When we bring individual atoms very
close together, the s- and p orbitals overlap
,making four mixed sp3 orbitals
(sigma bonding) created
S orbital allows 2 electrons occupy
P orbital allow 6 electrons occupy
n, l, m s
Streetman, p50
Valence electrons, i.e., the outmost electrons, in 3S and 3P orbital
could form bonding with atoms
of other materials
Electronic configuration and hybridized orbitals of Si

## Slide 4: 2s and 2p energy bands in a Li crystal
energy gap:
the intervening regions separating these bands
the area is forbidden
In general, the higher the band the greater
its width
-if the width of the band is 5 eV, there are 1023 level
, than the energy interval between two adjacent levels
Is only 5 x 10 -23
-for a<6a0 (lattice constant), the 2s and 2p bands
broaden to the point at which they begin to overlap
And the gap between them vanishes entirely. So lithium
has no band gap material under normal situation
2s and 2p bands for metallic Li plotted as
Functions of the lattice constant a
2p
2s
1s
2p
2s
1s
2p
2s
1s
-The evolution of the energy spectrum of
Li atom from an atom to a molecule and
to a solid
-The splitting of the 2p level is larger
than that of the 2s level, which is larger
still than that of the 1s level.
Atom
molecule
solid
forbidden
overlap
Energy band in a solid

## Slide 5: Energy level in a Si crystal
-Electronic configuration of Si: 1s22s22p63s23p2
-N Si atoms  2N, 2N, 6N, 2N, 6N states
3s-3p level contains 8N states (outer shell)
and split into 4N lower energy states (conduction band) and 4N higher energy states (valence band)
-N Si atoms have 4N outer electrons, at 0K, electrons only occupy in the 4N states in the valence band
Streetman, p59
Linear combination of atomic orbitals:
2 atoms, forming bonding and antibonding energy level

## Slide 6
Band gap schematic of Si

## Slide 7
Distinction between insulator, semiconductor and metal
Streetman p62
Insulator Semiconductor Metal
conduction band
valance band
> 5 eV
-very few electrons excited to
valance band at room temperature
-few electrons excited to conduction band
Ex, Si: 1010 / cm3
(note: Si has 5x1022 atoms/cm3)
plenty of
electrons

## Slide 8: Energy bands in solids
The behavior of an electron in a crystalline solid is determined by studing the
appropriate Schrodinger equation
- V(r) is the crystal potential seen by the electron.
According to Bloch theorem:
-all functions are vector functions, that is, with directions
-the vector k is a quantity related to the momentum of the particle

## Slide 9: Band structure in a semioconductor
Conduction band
Valence band
E=0
Simplest band structure of a semiconductor

## Slide 10
E-k diagram and energy band diagram

## Slide 11
Direct band gap and indirect band gap structure

## Slide 12: Carrier: electron and hole
Some electrons were excited to the conduction band at temperature >0K
For convenience, an empty state in the valence band is referred to as a hole
Electron-hole pair (EHP): conduction band electron and the hole are
created by the excitation of a valence band electron
-EHPs are free charge carriers in semiconductor materials
-Si, at room temperature has 1010 EHP/cm3 (Si: 5x1022 atoms/cm3)

## Slide 13
Carrier generated in the semiconductor under incident light excitation

## Slide 14: Carrier numbers in intrinsic material
n = number of electrons/cm3
p = number of holes/cm3
n=p=ni
ni=1010/cm3 in Si at room temperature
1013/cm3 in Ge at room temperature
Si has 5 x 10 22 atoms/cm3, with four bonds per atoms
2 x 1023 valance band electrons
Less than one bond in 1013 broken in Si at room temperature
That is why need to dope Si and Ge

## Slide 15: Doping
Donors: P, As, Sb (Column V elements ) , n-type,  provide one additional electron
Acceptors: B, Ga, In, (Column III elements), p-type provide one additional hole
P+
B-
-
-weakly bound
-bonding strength EB~ 0.05 eV (Si bonding ~1.12 eV)
Majority carrier - electron in a n-type material
hole in a p-type material
Minority carrier – hole in a n-type material
electron in a p-type material

## Slide 16
N-type Semiconductor schematic

## Slide 17
p-type Semiconductor schematic

## Slide 18: ED donor levels to the energy band diagram
Donors EB Acceptors EB
Sb 0.039 eV B 0.045 eV
P 0.044 eV Al 0.057 eV
As 0.049 eV Ga 0.065 eV
In 0.16 eV
Ec
Ev
ED
0.044 eV (P)
0.057 eV (Al)
EA
T=0 C
Increase T
Group V
Group III

## Slide 19: Density of states
Energy distribution of allowed states in each band
Tells one how many states exist at a given energy E
g(E)dE: the number of conduction band states/cm3 lying in the
energy range between E and E+dE
E
Ec
Ev
gc(E)
gv(E)
gc(E) is zero at Ec, and increases as the square roote
of energy when on proceeds upward into the conduction
band
The same as gv(E)
gc(E)dE: represents the number of conduction band
states/cm3 lying in the energy range between
E and E+dE (If E
Ec)
more
states
more
states

## Slide 20: Fermi function
Fermi-Dirac distribution function for a electron
At fermi level, occupation probability is 1/2
-EF=Fermi energy or Fermi level
-specifies how many of the existing states
at the energy E will be filled with an electron
-that is, under equilibrium conditions, the
probability that an available state at an energy
E will be occupied by an electron
-simply a probability density function
EF+3kT
EF-3kT
-at room temperature, kT~0.026 eV and 3kT ~0.078 eV (Si’s EG: 1.12 eV)
Compared to Si band gap, the 3kT energy interval that appears prominently
In the T> 0 K is typically quite small
-So, there is very low probability of electron appear in conduction band at room temperature

## Slide 21: Representation of intrinsic, n-type, p-type semiconductor materials using the energy band diagram
Ec
Ei
Ev
Ec
EF
Ei
Ev
Ec
Ei
EF
Ev
Intrinsic n-type p-type
fermi level shift

## Slide 22: Equilibrium distribution of carriers in intrinsic and doped semiconductors
g(E)
hole 1-f(E)
The concentration of electrons in
the conduction band
most carrier concentrations
near the band edges
The concentration of holes in
the valence band

## Slide 23
Color schematic

## Slide 24: Carrier action
Drift:
electrons and holes move due to a electrical field E
Diffusion
electrons and holes move due to concentration gradient
E
+ -
Recombination - generation
Ec
Ev
heat or light

## Slide 25: Drift current
I (current) = the charge per unit time crossing an arbitrarily chosen plan
for electron drift In,drift=qnvdA –electron drift current
Jn,drift= I/A=qnvd vd (constant drift velocity)
Vd=μxE
Jn,drift= qμnnE
Jp,drift= qμppE
Un~1360 cm2/V-sec in ND=1014/cm3 doped silicon
Up~490 cm2/V-sec in NA=1014/cm3 doped Silicon
μ: mobility, cm2/V-sec

## Slide 26: Diffusion on a microscopic scale in a hypothetical one-dimensional system
1024
512
512
512
256
256
384
384
128
128
320
256
256
192
: the number of particles
In a given compartment
t=0

## Slide 27: Diffusion currents/total carrier currents
Jp=qμppE - qDp
p
Jn=qμnnE + qDn
n
drift
diffusion
Total carrier current combined with diffusion and drift

## Slide 28: Carrier recombination – generation (R-G)
light
heat
heat
Ec
Ev
Ec
Ev
Ec
Ev
Ec
Ev
-
light
heat
-
-
+
-
+
x
x
x
ET
photogeneration
Direct thermal
generation
Direct thermal
recombination
Recombination
and generation
From indirect thermal
recombination-generation
process
R-G centers
The termal creation and anihilation of carriers typically dominated by indirect
thermal-generation
-R-G centers (ET) are impurity atoms (gold in Si) or lattice defects, can trap
carrier easily
-like a trap

## Slide 29: R-G statistics
-The rate of change in the carrier concentration
perturbation
△P
n~no
△p<<no
Low level injection implied
△p<<no n~no in an n-type material
△n<<Po p~po in an p-type material
n-type semiconductor
A technical men given to the mathematical characterization of recombination-generation process
R-G evaluates the time rate of change in the carrier concentrations
Ec
ET(R-G)censter
Ev

## Slide 30: n-type semiconductor after a perturbation
t=0
P0
n-type semiconductor
t>0
perturbation
△P
n-type semiconductor
t->infinite
perturbation
△P=0
n-type semiconductor
The change of minority carriers
dominate the recombination rate
Ec
EF
ET(R-G)censter
Ev
n~no
po
△P<<no
To be approximately
Proportional to △P
(R-G)
For holes in a n-type material;
(R-G)
To be approximately
Proportional to NT (R-G center numbers)
For electrons in a
p-type material
(since the multitude of electrons rapidly
fill any level that is vacant)
The more holes available for
annihilation, the greater
the number of holes recombining
per second.
(R-G)
Cp Cn is a positive proportionality constant
(R-G)

## Slide 31: Minority Carrier lifetimes
For holes in an n-type material
For electrons in an p-type material
-are called minority carrier lifetimes ; interpreted as the average time
an excess minority carrier will live in a sea of majority carriers
-In a Si with very few R-G center, lifetime is around 1 msec
- Typical minority carrier lifetimes in most Si device is around 1 μsec
We introduce the time constants
Diffusion lengths
hole in an n-type material
electron in a
p-type material
(R-G)
(R-G)

## Slide 32: Charge neutrality
In a semiconductor with equilibrium state.
the charge should be neutral, otherwises,
there occurs an electric field
qp – qn + qND - qNA = 0
+
-
ND+ = number of positively charged donor sites
NA- = number of negative charged acceptor sites
Charge/cm3

## Slide 33: Carrier Related terminology
Dopants: specific impurity atoms which are added to semiconductors in controlled amounts for the expressed purpose of increasing either the electron or the hole concentration
Intrinsic semiconductor: undoped semiconductor; a semiconductor whose properties are native to the material
Extrinsic semiconductor – doped semiconductor; a semiconductor whose propeties are controlled by added impurity atoms
Donor – impurity atom which increase the electron concentration; n-type dopant.
Acceptor – impurity atom which increase the hole concentration; p-type dopant
N-type material – a donor-doped material; a semiconductor containing more electrons than holes
P-type material – an acceptor-doped material; a semiconductor containing more holes than electrons
Majority carrier – the most abundant carrier in a given semiconductor sample; electrons in an n-type materials, holes in a p-type material.
Minority carrier – the least abundant carrier in a given semiconductor sample; holes in an n-type material, electrons in a p-type material.