## Slide 1
Fundamentals of Optoelectronic Materials and Devices 光電材料與元件基礎
Hsing-Yu Tuan (段興宇）
Department of Chemical Engineering, National Tsing-Hua University

## Slide 2
PN junction:summary
E=-dV/dx
charge density
potential
Story:
The carrier concentraion
difference between the n and p
regions causes the carriers to
diffuse. The diffusion, however,
Leads to a charge imbalance.
the charge imbalance in turn
produces an electric field, which
counteracts the diffusion so that
in thermal equilibrium the net
flow of carriers Is zero.
The charged region near the
metallurgical junction where
the mobile carriers have been
reduced is called the depletion
region
Vo: built-in-potential
no carrier in the
depletion region

## Slide 3
Forward and reverse bias effect for a pn junction
Fermi level equilibrium
Forward bias reduces the eVo to
e(Vo-V), so the electrons at Ec
in the n-side can overcome the the
potential barrier and diffuse to the p-side
A reverse bias, V=-Vr, Vr adds to the
built-in potential Vo, so the P.E barrier
becomes e(Vo+Vr), so there is hardly any
reverse current.

## Slide 4: Fabrication of Light Emitting Diode using a pn junction structure

## Slide 5
Light Emitting Diodes: Principle
made by a junction consists of p-side with heavily-n-doped-side (n+)
Depletion region extends mainly into p-side
built in voltage
the recombination of injected electrons in the depletion region as well as in the
neutral p-side and results in spontaneous emission of photons
-the recombination zone is called the active region
-light emission from EHP recombination as a result of minority carrier injection
is called injection electroluminescence

## Slide 6
-P-layer has to be narrow (a few microns) to allow the emitted photons escape
without being reabsorbed
LED device structure
Narrow

## Slide 7
LED device structure
p
GaAs is around 160

## Slide 8
LED device illustration

## Slide 9: LED semiconductor materials
ηexternal = Pout (optical) x 100%
IV
1993 年日亞(Nichia)發展高效率藍光LED!

## Slide 10
LED materials – mainly III-V based direct band gap
materials
- II-VI compounds are hard to be doped, so not usually be used

## Slide 11
Evolution of light source

## Slide 12
Tuning band gap by alloying or doping
y=0.45, λ=630 nm
Red light
Nitrogen doped indirect bandgap GaAs1-yPy allows can emit green, yellow, orange LEDs
Al doped SiC, GaN are can emit blue emission, however, Al doped SiC is indirect band gap
and GaN is very expansive
Alloy
doping

## Slide 13: LED characteristics
The energy of an emitted photon from an LED is not equal to the Eg
Electron (hole) concentration’s peak position is 1/2kBT above Ec or Ev
and direct recombination is proportional to the concentration
-The linewidth is defined as width between half-intensity equal to △hv , normally
is around 2.5-3 kBT
E=hv

## Slide 14
Output spectrum of a red GaAsP LED
- =24 nm is around 2.7kBT
-Turn-on voltage increase with the energy bandgap Eg, vlue LED is 3.5-4.5 V
yellow LED is around 2 V, GaAs infraed LED is around 1 V
Turn-on voltage:1.5V

## Slide 15
Peak emission

## Slide 16: White light LED
White light for lighting – long service life, electricity effective, low driving voltage, safe
White light LED:
First example: Blue LED + YAG (yttrium aluminum garnet, 釔鋁石榴石) yellow phosphor (currently most popular, low cost & high efficiency) (at 1996)
- RGB LEDs (Red:green:blue = 3:6:1)
- UV LED (GaN) + RGB phosphors

## Slide 17: Various combination of white LED

## Slide 18: Evolution of light source
LED has 80% lower energy vs. incandescent
LED has 39% lower energy vs. CFL
Courtesy of Osram
compact fluorescent light
Efficiency now is
the best.

## Slide 19: Light output V.S. Efficiency

## Slide 20: Cost comparison of light bulbs

## Slide 21: Cost comparison of light bulbs

## Slide 22: Is the technology revolution similar?

## Slide 23
High tech product combined with LED
水立方

## Slide 24: Fabrication of laser diode using pn junction structures
Laser: Light Amplification by Stimulated Emission of Radiation

## Slide 25: Two keys for making a laser
population inversion
Optical cavity

## Slide 26: Absorption, spontaneous, and stimulated emission
Emission: an electron at a higher energy level transits down to an unoccupied energy level
and it emits a emits a photon
Spontaneous emission: emitted photon from E2 to E1 in a random direction, which
provided by the E1 not already occupied by another electron
Stimulated emission:
Emitted photon is in phase with incoming photon
(the same direction, the same energy, the same polarization)
Incoming photons was magnified there are more atoms at E2 than
at E1 (population inversion), so incoming photons were not absorbed
by another atom at E1
The key 1 of laser: population inversion

## Slide 27
The way to achieve population inversion
Note:
-in normal case, only two energy levels can not achieve population inversion
-external excitation first excite electron from E1 to E3
-the emission from E2 to E1 is called lasing emission
-LASER: Light Amplification by Stimulated Emission of Radiation
- an example: Cr+3 ion in a crystal of alumina Al2O3 (saphire)

## Slide 28
Er+3 doped glas fiber : an example

## Slide 31: Make Stimulated emission rate larger
R21 - downward transition rate from E2 to E1
We need a large photon concentration
with the wavelength we want!
- Need an optical cavity
-photon energy density per unit frequency
-the number of photons per unit volume with an energy hv=(E2-E1)
stimulated
spontaneous
R21 = A21N2+B21N2 (hv)
Spontaneous emission
Stimulated emission which requires
Photons to drive it
Spontaneous emission
Stimulated emission

## Slide 32: A optical cavity (optical resonator)
-We build a optical cavity to trap the wavelength
we want
-only standing waves with certain wavelength
can be maintained within the optical cavity
m:mode number (an interger)
Wavelength satisfy the left equation is called
A cavity mode

## Slide 33: Laser diodes: utilization of PN junction
Compared to other lasers (sapphire, CO2, HeNe, dye), semiconductor laser diodes are compact in size, electricity effective, efficient, long life, cheap, and versatile in color from UV to IR.
Applications – CD,VCD,DVD players, CDROM, laser printer, laser pointer, bar code scanner, etc.

## Slide 34: Degenerated semiconductor
the semiconductor that was excessively doped with donors or acceptors (1019-1020 cm-3) called degenerate semiconductor
such a semiconductor exhibits properties that are more metal-like
-degenerate doping: the Fermi level EFP in the p-side is in the valence
band(VB) and the EFn in the n-side is in the conduction band (CB)
-a laser diode consists of “degenerately” doped p+ side with “degenerated”
doped n+ side (p+n+ junction)

## Slide 35
Structure: degenerately doped direct bandgap semiconductor pn junction
laser diode structure: degenerately doped direct bandgap semiconductor pn junction
depletion region (active region) is very narrow
population inversion occurs when applying a voltage larger eV > Eg:
the applied V diminishes the built-in potential to zero and electrons flow into the SCL
an incoming photon with energy Ec-Ev doesn’t excite an electron but stimulated by
falling electrons
After applying large forward
bias V
LED

## Slide 36
Density of States and optical Gain in the active layer
the active region has an optical gain since an incoming photon is more likely
to cause stimulated emission than being absorbed
-the pumping mechanism caused by forward diode current is called injection pumping
-the pumping energy is supplied by the external battery

## Slide 37
Build an optical resonator in a laser diode
-an optical cavity (resonator)) is required to implement a laser oscillator to build up the intensity of stimulated emissions.
-the ends of the crystal are cleaved to be flat and optically polished to
provide reflection and form an optical resonator
-this process can build up the intensity of the radiation in the cavity
an optical resonator
n: refractive index

## Slide 38: Output power vs. diode current of a laser diode
-lasing radiation is only obtained when the optical gain in the medium can
overcome the photon losses from the cavity, which requires the diode current I
to exceed a threshold value Ith
-below Ith: spontaneous emission; above Ith: stimulated emission
Threshold current

## Slide 39
Comparison of laser’s and LED’s light power versus current

## Slide 40: Heterostructure laser diode
a heterostructured laser diode can significantly reduce the threshold current (Ith)
-we confine the injected electrons and holes to a narrow region, so that
less current is needed to make population inversion
-carriers are confined in the p-GaAs (active area) when the voltage is applied
-gaAs layer is very thin, so the concentration of injected electrons can be increased
quickly with moderate increases in forward current.
+
+
+

## Slide 41
Schematic illustration of a double heterojunction laser diode

## Slide 42: photovoltaic device (solar cell)

## Slide 43: Solar cells
Solar light in
Electricity out

## Slide 45: Generate electrons from materials by photons
Semiconductor, polymer or dyes
Separation of the
electron-hole
pair
Conduction band
or HOMO
Valence band
or LUMO
Conduction band
or HOMO
Valence band
or LUMO
electron
pair
So, materials used for solar cell application need to have discrete energy
gap for photogeneration of electron-hole pair
excited state

## Slide 46: Elemental and Compound Semiconductors
 |  | 5 B | 6 C | 7 N | 8 O
 |  | 13 Al | 14 Si | 15 P | 16 S
29 Cu | 30 Zn | 31 Ga | 32 Ge | 33 As | 34 Se
47 Ag | 48 Cd | 49 In | 50 Sn | 51 Sb | 52 Te
I II III IV V VI
46
Notes: 46
You have heard many good things from me about CIGS solar cell. From here, I would like to give a brief introduction of CIGS material and its properties. CIGS is a I-III-VI compound semiconductor derived from II-VI compound. The group II element is replaced by group I and group III elements. Therefore, the I-III-VI compound has the atomic ratio of 1:1:2. Like other compound semiconductors, the elements belongs to the same group can be substituted to form solid solution such as Cu-In-Ga-Se quaternary compound or even Cu-In-Ga-Se-S pentanary compounds.

## Slide 47: Definition of various radiation
AM0 ：太陽光在大氣層外的平均照度稱為AM0，其功率約1300W/m^2
AM1 (90 °) ：太陽光透過大氣層後與地表呈90度時的平均照度稱為AM1，其功率約925W/m^2
AM1.5 (45 °)： AM1.5用來表示地面的平均照度，是指陽光透過大氣層後，與地表呈45°時
的光強度，功率約844W/m^2，在國際規範(IEC 891、IEC 904-1)將AM1.5
的功率定義為1000W/m^2。
photovoltaic = photon + voltaic
m=h/ho=secθ

## Slide 48: Pick right materials
- Good absorption coefficient to harvest
light
- Suitable band gap

## Slide 49: Absorption of semiconductors
Phonon emission o
r absorption
-We prefer direct semiconduct materials
since they can absorb light more efficiently
-Si and Ge’s absorption coefficient
increase slowly with increased energy

## Slide 50
Theoretical maximum efficiency of a semiconductor
S(λ) =# of photons/area*time
bandgap of semiconductor should not be wide
get higher S(λ)
-Electrons in the valence band can absorb energy of Eg, 2 Eg, 3Eg, but the excess energy can not be transformed to electric energy but transform to heat  need higher Eg
-very narrow band gap material can absorb most wavelength from sun, but transformed energy is small.
Pick suitable Eg (eV)

## Slide 51
real ηmax is only around
30% due to loss of other facters
ηmax(%) vs Eg (eV) under AM1.5
Eg:
1.0 – 1.5 eV is the best range

## Slide 52: Absorption of semiconductor
Phonon emission o
r absorption
-We prefer direct semiconduct materials
since they can absorb light more efficiently
-Si and Ge’s absorption coefficient
increase slowly with increased energy

## Slide 54: A PN junction photovoltaic device
-incoming photon generate EHPs and
separated by the build-in field Eo, drifts them apart
-generated electrons and hole can
diffuse and drift in neural region and SCL, respectively
-

## Slide 55: A PN junction photovoltaic device
-The movement of minority carriers is critical for
the amount of generated current
-Without Eo it is not possible to drift apart
the photogenerated EHPs accumulate
excess electrons on the n-side and
excess holes on the p-side

## Slide 56: A PN junction photovoltaic device
:life time
Only electrons within the Le to the depletion
Layer can contribute to the photovoltaic effect
-Silicon’s electron diffusion length is longer than
the hole diffusion length
-we make a device with very narrow n region and
longer p region
-n side: 0.2 μm or less ; p-side: 200-500 μm
Reason: (1) the electron diffusion length in Si
Is longer than the dole diffusion length
(2) At long wavelengths, around 1-1.2 μm, the
absorption coefficient α of Si is small and the
absorption depth (1/ α) is typically greater than 100 μm.
Electron diffusion length
200-500 μm
0.2 μm

## Slide 57
Photocurrent Iph = eGoA(ln + W+Le)
Photogenerated carriers within the solar cell
Go = photogeneration rate
At

## Slide 58
Device structure of a Si solar cell
and to allow more photons into the device
Finger electrodes
p
n
Bus electrode
for current collection
- finger electrodes were made to allow light pass through the device
a thin antireflection coating on the surface reduces light reflection and allow more
lighte to enter the device
-surface texturization to for multiple light reflection and increase light path
0.2 μm
200 μm
In order to capture more light
surface texturization
Incident light
(1)
(2)
(3)